New Developments in Thermoplastic Elastomers: The Hard Segment Inelastic Effects OnThe Mechanical Performance of Polyurethane Elastomers

C. Prisacariu*, E. Scortanu, Institute of Macromolecular Chemistry “Petru Poni, Iasi, 700487, Romania; Email: crispris@icmpp.ro

C.P. Buckley, Department of Engineering Science, University of Oxford, OX1 3 PJ, Oxford, UK

Abstract— A study was made of a series of polyurethane copolymers (PUs), in which the chemical components were: a hard segment (giving, on phase separation, hard nano-scale reinforcing particles); a soft segment (giving, on phase separation, an elastomeric matrix), and a diol chain extender. (PUs) were investigated, based on several diisocyanates of rigid and/or variable geometries, with the aim of improving understanding of the relationship between molecular/supramolecular architecture at the nm-scale and macroscopic mechanical properties in such systems. A novel diisocyanate (4,4’-dibenzyl diiscyanate (DBDI)) and a triol chain extender (1,1,1-trimethylol propane (TMP)) were included as well as more widely-used components, in order to widen the range of structures achievable beyond those normally available. The chemical changes, and variation of thermal history, lead to varying degrees of phase segregation and crystallization in the hard segment, particularly when using DBDI which displays a variable geometry due to which there result PUs with increased degrees of crystallinity. Rotation around the central –CH2-CH2- bond in DBDI allows alignment of successive aromatic rings thus favoring the tendency of crystallization which involves the DBDI hard phase. The chemical compositions of were varied systematically and independently, and their mechanical responses were measured in cyclic tensile tests at room temperature, up to stretches in the range 5-6. Particular attention was paid to characterizing the inelastic features – hysteresis, and stress relaxation in interrupted tests – and their variations between the materials. The same materials were also studied by wide-angle X-ray scattering (WAXS) and differential scanning calorimetry (DSC), to determine levels of crystallinity. Results showed that hysteresis was increased by increasing hard phase crystallinity. The extent of stress relaxation in interrupted tests was found to increase with hysteresis and hence with hard segment crystallinity, reflecting the higher flow stress of the reinforcing hard domains. In large deformation cyclic experiments at room temperature, the degree of hysteresis and stress relaxation were found to be greatly enhanced by hard-phase crystallinity, through its effect of increasing the flow stress.

Speaker: Dr. PRISACARIU  CRISTINA

i. CV.

AFFILIATION AND OFFICIAL ADDRESS:

The Romanian Academy’s Institute of Macromolecular Chemistry “Petru Poni”, Iasi,

Aleea Grigore Ghica Voda, Nr. 41 A, 700487, Iasi, Romania

DATE AND PLACE OF BIRTH:02/07/1959, Iasi, Romania

NATIONALITY:  Romanian

EDUCATION / KEY QUALIFICATIONS / POSITIONS HOLD:

1978, Graduate with honours “G.. Ibraileanu” High School, Specialization: Mathematical/Physical Sciences

1977- 1980 Graduate with honours The “School of Arts, Picture and Graphics”, Iasi, Romania

1983, Graduate with honours in Engineering, “Gh. Asachi” Technical University Iasi, Romania

1983-1989,“C. Negruzzi” High School, Iasi, Romania, Teacher of Technical Disciplines,

1989,The Romanian Academy’s Institute of Macromolecular Chemistry “Petru Poni”, Scientific

researcher,

1999 PhD Title in Materials Science / Polymer Mechanics / Strength of Materials  - , (25/06/1998), “Gh. Asachi” Technical University Iasi, Romania- Faculty of Architecture and Civil Engineering; PhD thesis title “New insights towards the physical/mechanical properties of   polyurethanic materials” (graduate with honours).

- 1998, appointed as a Senior Researcher (the equivalent of a Lecturer position) at The Romanian Academy’s Institute of Macromolecular Chemistry  “Petru  Poni”, Iasi, Romania

- 2001, Senior scientist, the (equivalent or a Reader position), The Romanian Academy’s Institute

of  Macromolecular Chemistry “Petru  Poni”, Iasi, Romania

PROFESSIONAL EXPERIENCE / SPECIALIZATION

A. Specialization in teaching:

- Experience as a Teacher of Science, 1983-1988,“C. Negruzzi” High School, Iasi, Romania;

Teaching /training courses of Technology and Strength of Materials for staff etc. at The Institute of  Macromolecular  Chemistry „Petru Poni“, Iasi

B. Specialization as a researcher: macromolecular/ polymer materials; polymer mechanics, polymer chemistry.

Responsabilities: 1988-2004: Head of Department of Mechanical testing of Polymers / Institute of Macromolecular  Chemistry „Petru Poni“, Iasi

Specialization as a researcher

1988-present: Polymer characterization; knowledge transfer and consultancy in mechanical testing of polymers as part of previous contracts between institute and industry and army where I was in charge with the products quality control.

1988-present: Synthesis and characterization of polyurethane films, coatings and composites;    study of the physical/chemical properties and mechanical  behaviour  of: elastomers, polymers based on complex isocyanate structures, multiphase systems of polyurethane elastomers, films, blends and polyurethane coatings.

2000-2001 Dichroic infrared studies on polyurethanes; monitoring of  changes of IR signals;

2000-present: Synthesis of polyurethanes based on isocyanates of variable geometry

2004-present:Study of environmental impact in poyurethanes of different structures

2004-present: Study of the constitutive response and modelling of polyurethanes deformation and dependence of structure

Publications and other activities: 44 papers (in journals with impact factor), participation with more than 100 contributions (3 key lectures,14 lectures and international conferences, 6 oral presentations, 7 seminars and posters) at international and national symposia, 1 book and 1 chapter in a book.

Participation at 4 national grants (as a Project Leader).

Participation at 3 international grants from 2003 to 2008 (2 of which as a Romanian project leader) – as detailed below.

PARTICIPATION IN PAST AND CURRENT RESEARCH PROJECTS

A. International research projects

- Overseas Romanian Project Leader as part of a UK Royal Society Joint Project between The Institute of Macromolecular Chemistry “Petru Poni”, Iasi, Romania and The Department Engineering Science, University of  Oxford, UK, 2003 -2005; title of project “Optimising performance of  polyurethane elastomeric products via control of chemical structure” .

- Project Coordinator / principal investigator  as part of an ongoing NATO Collaborative Linkage Grant, 2005 – 2008, Project nr: PDD(CBP.EAP.CLG 981805/ 22.07.2005) between The Institute of Macromolecular Chemistry “Petru Poni”, Iasi, Romania and The Department Engineering Science, University of  Oxford, UK; title of project „ New polyurethanes and the nano-structural origin of their stress-strain response”;

- Co-investigator as part of an “ISIS / CCLRC” project; Nr. 510315 / 2004

(same partner as above); title of project: “The nano-structural origin of the constitutional response in segmented co-polyurethane elastomers“

B. National Research projects

Project leader of 4 National Romanian projects funded by the Romanian Academy, as follows: Romanian Academy Grants:  GAR 41/2003; GAR 31/2004; GAR 59/2005; GAR 41/2006 (detailed titles etc can be submitted if requested)

SCHOLARSHIPS / CONFERENCE GRANTS

- 1994, Soros – Oxford University Fellowship, at The Dept of Materials / Dept. of Engineering

Science, University of Oxford

- 1999,European Science Foundation (ESF) grant /ESF programme (SUPERNET), Strasbourg

- 2000, Cooperation Exchange 2000 via an Eureka grant, Brokerage Event COPEX 2000, organised

in the frame of Cordis, FP5 Fifth Framework Programme, June,Vienna 2000.

- 2000, Martin Luther University Halle/Saale, Wittenberg, German DFG conference grant,

“Polymeric Materials/ P2000” event, September

- 2002, Martin Luther University Halle/Saale, Wittenberg, German DFG conference grant,

“Polymeric Materials/ P2000” event.

- 2004, Organization for the Prohibition of Chemical Weapons (OPCW),The Hague, The

Netherlands conference grant to attend “11th International Conference in Polymers and Organic

Chemistry, POC ’04”, Prague, Czech Republic, July, 2004

-- 2004, Martin Luther University Halle/Saale, Wittenberg, German conference grant, “Polymeric

Materials/ P2000” event, September 2004.

- 2005, PPS-21 conference grant supported by DFG, Germany.

-  2006, Martin Luther University Halle/Saale, Wittenberg, German conference grant, “Polymeric

Materials/ P2000” event, September 2006.

FELLOWSHIPS AND POSTDOCTORAL POSITIONS WITHIN INTERNATIONAL RESEACH PROJECTS

- 2000, UK Royal Society fellowship at The Engineering Science  Dept, University of  Oxford

- 2001, DAAD German fellowship, The Institute of Polymeric Materials e.V., Merseburg / Martin

Luther University of Halle, Wittenberg, Germany

-2001, UK Royal Society fellowship at The Engineering Science  Dept, University of  Oxford

- UK Royal Society fellowship via a Joint Project at The Engineering Science  Department,

University of  Oxford, UK, 2003

- UK Royal Society fellowship via a Joint Project at The Engineering Science  Department,

University of  Oxford, UK, 2004

- NATO fellowship via a NATO CLg collaborative linkage grant, at The Engineering Science

Department, University of  Oxford, UK, 2005.

- NATO fellowship via a NATO CLg collaborative linkage grant, at The Engineering Science

Department, University of  Oxford, UK, 2006.

-  NATO fellowship via a NATO CLg collaborative linkage grant, at The Engineering Science

Department, University of  Oxford, UK, 2007.

- Chairperson at the Polymer Processing Society Meeting (PPS-21), Leipzig 2005.

ii. (a) Selection of publications and proceedings:

1. Caraculacu A., Agherghinei I, Gaspar M, C. Prisăcariu, “A New Method for a Kinetic Study of Reactions between Di-isocyanates and Alcohols. Part I. Symmetrical Di-isocyanates”, J. Chem. Soc. Perkin Trans. 2, 1343,(1990)

2. Caraculacu, A., Aghreghinei, I, C. Prisăcariu,  and Cozan, V. “Dibenzyl Structures in a Macromolecular Chain III. Dibenzyldiisocyanates Reactivity”, J. Macromol. Sci.- Chem., A 27 (12), 1547 - 1570, (1990)

3. Agherghinei, I., C. Prisăcariu and Caraculacu A.A.., “A New Method for a Kinetic Study of Reactions Between Diisocyanates and Alcohols. PartII. AsymmetricalDiisocyanates: 2,4 - toluylene diisocyanate”, Rev. Roumaine de Chimie, 36,9-10,1135-1145,(1991)

4. Horbaniuc, D., PrisăcariuCr.Bauşic, V. şi Caraculacu, A.,“Structuri dibenzilice pe lanţul macromolecular Variaţia rigidităţii elastomerilor poliuretanici cu structură  dibenzilică  în cazul solicitărilor statice de torsiune la temperaturi scăzute” , Rev.Materiale Plastice. 33, Nr.3.,168 - 176, (1996).

5.Prisăcariu Cr., Caraculacu, A.A. and Williams Br. “Dibenzylic Structures on the Macromolecular Chain. X. Maturation Phenomena in Casting Polyurethane Elastomers Synthesis”, Polytechnical Inst. “Gh. Asachi”, Bull. Iasi - Issue XLII, (XLVI), 3-4, (1996), Section I. Matemathics. Theoretical Mechanics. Physics. (1996), pag.123-135.

6.C. Prisăcariu, I. Agherghinei, “Reaction in solid state within polyurethanes. Kinetics and  postcure reaction  mechanism in casting polyurethane elastomers”, J.M.S.-Pure Appl. Chem.,  A37  (7), 785 -  806 (2000)

7. C. Prisacariu , R.H.Olley, A. Caraculacu, D.C.Bassett and C. Martin, “The effect of hard segment in copolyurethane elastomers obtained by using simultaneously two types of Diisocyanates”, Polymer 44, 5407-5421 (2003).

8. C. Prisacariu, C.P. Buckley C.P., A. Caraculacu – „Mechanical response of dibenzyl-based polyurethanes with diol  chain extension” –  Polymer 46, 3884-3894, (2005)

9. C. Prisacariu, Buckley C.P, Caraculacu A, PU Deutsche Magazin ,4, 253- 258., (2006).

10 .C. Prisacariu, Thermal Analysis of Novel Nolyurethane Block Polymers Derived From Flexible Hard

Segments,      Polytechnical Inst. “Gh. Asachi”, Bull. Iasi – Vol. XLVII,(LI), 1-2, Section I. Mathematics. Theoretical       Mechanics. Physics, 143-156, (2001).

11..A. Caraculacu and C. Prisacariu, The influence of The Hydrogen Bonding on The Polyurethane Elastomers  Mechanical Performance I.Hydrogen  substitution with inert groups and isotope effects, Polytechnical Inst. “Gh. Asachi”, Bull. Iasi - Vol XLVII, (LI), 1-2, Section I. Mathematics. Theoretical Mecanics. Physics, 129-143, (2001).

12.C. Prisacariu, Influence of Polymer Network on The Compression Properties of Novel Polyurethane Elastomers Based on Complex Hard Segments with Conformational Mobility, Polytechnical Inst. “Gh. Asachi”, Bull. Iasi – Vol. XLVII, (LI), 3-4, Section I Mathematics. Theoretical Mecanics  Physics, 106-118 (2001).

13.C.Prisacariu, A. Caraculacu, The Effect of Intramolecular Order in Block Copolyurethane Elastomers. I. Stress Strain, Stress Relaxation and The Energy Loss, The 6th  International Conference on Residual  Stresses, Institute of Materials The Royal Society, Londra, Marea Britanie, Oxford, 10-12 July 2000, 415-423, (2000).

14.C. Prisăcariu, A. Caraculacu, Isotope Effects on the Dibenzyl Polyurethane Elastomers Deformation  and  Fracture - 11th International Conference on “Deformation, Yield and Fracture of Polymers, Institute of  Materials - The Royal Society, Londra, Marea Britanie, Cambridge,10-13 Aprilie 2000, 458-461, (2000).

15. C.Prisacariu, A. Caraculacu, Time, Deformation and Fracture in Dependence in Dibenzyl Casting Polyurethane Elastomers – 11th International Conference on “Deformation, Yield and Fracture of Polymers, Institute of  Materials - The Royal Society, Londra, Marea Britanie, Cambridge,10-13 Aprilie 2000, 462-465, (2000).

16. C.Prisacariu, A.Caraculacu,-Phase Separation and Crystallisation Phenomena In Polyurethane Elastomers Based on Hard Segments with Variable Geometry, “Polymeric Materials 2000”,Halle/Saale,  25 –27 September 2000, Germania, 473-476, (2000).

17. C.Prisacariu, A.Caraculacu,The effect of Hard Segment Conformational Mobility on The Polyurethane  Elastomers  Deformation and fracture behaviour, “Polymeric Materials 2000” ,Halle/Saale,  25 –27 September 2000, Germania, 235-239, (2000).

18.C. Prisacariu, A.Caraculacu, Novel polyurethane films with a coplanar packing in the hard segments: from

synthesis to optimisation of mechanical performance,  8th International Seminar on Elastomers, 9-11 May, 2001, Le Mans, France, 278-280, (2001).

19. C. Prisacariu, A. Caraculacu, The effect of hard segment distribution and ordering in two types of diisocyanates  based copolyurethane elastomers, 8th International Seminar on Elastomers, 9-11 May, 2001, Le Mans, France, 281-283, (2001)

20 C. Prisacariu, A. Caraculacu, Structural architecture effects of novel block copolymer polyurethanes on the      elastomeric mechanical performance, 8th International Seminar on Elastomers, 9-11 May, 2001, Le Mans, France,     284 -286, (2001).

21. C. Prisăcariu, A. Caraculacu, The Effects on Polzurethane Elastomers Thermal Behaviour Due to Varying

Crystallinity by the Hard Segment Variable Geometry, “Polyurethanes 2002” Division of Polymer Chemistry      Meeting, Annapolis, Maryland, Sept.29-Oct.2, 2002; Pres. Number 10.

22.C.P.Buckley, C.Prisacariu and A.A. Caraculacu, Constitutive response of model segmented copolyurethane     elastomers, Euromech Colloquium and Workshop, Vienna, July 2002,96-99 (2002).

23. C.P.Buckley, C.Prisacariu and A.A. Caraculacu, Effects of hard segment crystallinity on constitutive response of copolyurethane elastomers, submisa la 12th International Conference on Deformation, Yield and Fracture of  Polymers, Cambridge, UK, 7-10 April 2003, 349-352.

24. C.Prisacariu , C.P.Buckley, A. Caraculacu, “Novel polyurethanes with tailored properties induced by differences  in Crystallinity”, Chem Bull “Politehnica” Univ. Timisoara, 48 (62), 1-2, 2003, 53-56.

25. C. Prisacariu, C.P. Buckley, S. Ilisch, A. Caraculacu, “Structural modifications in novel thermoplastic polyurethanes  as revealed by static and dynamic tensile testing as a function of temperature”, Chem Bull “Politehnica” Univ. Timisoara, 48 (62), 1-2, 2003, 57-60.

26. E. Scortanu, C. Prisacariu, A. Caraculacu,”Study of the mechanical properties of dibenzyl-based polyurethane containing a molecularly dispersed UV absorber”, High Performance Polymers, 16, (1), 113-121 (2004).

27..Prisacariu C, Buckley C.P., Caracualcu A.A. – „Mechancial response of dibenzyl-based polyurethanes with dil   chain extension” –  Polymer 46, 3884-3894, (2005)

28. Prisacariu C, Caraculacu A, - „The influence of ageing conditions and chemcial structure on the stress-strain data   of dibenzyl based polyurethane films” –  Bul. Inst Polit.iasi, t.L1 (LV),f.1,  Sectia Stiinta si Ingineria Materialelor., 9-15, (2005)

29. Scortanu E, Taranu A, Prisacariu C,  Caraculacu A.A., - "Heterocyclic Polyurethanes. Intermolecular interactions   as revealed by GPC and viscosity measurements", Analele Stiintifice ale  Universitatii "Al. I. Cuza" din Iasi, Tom

XIV, Nr. 1, 51-57 (2006).

30. Prisacariu C., Buckley C.P.,  Prisacariu V.A, - „Particular aspects on the deformation and fracture of novel   dibenzyl polyurethane elastomers of variable crystallinity” ,  Bul.Inst. Polit., Iaşi, Fasc.1,Secţia Ştiinţa şi Ingineria  Materialelor, 34-40, (2006)

31. Scorţanu E, Prisacariu C, Caraculacu A, M.Brumă, N. Suliţanu - „New heterocyclic polyurethane-ureas based on

4,4'-dibenzyl diisocyanate. Part 1. Influence of oxadiazole structure on mechanical properties” , High Perform.

Polym. 18 (2), 127-143, (2006)

32. Prisăcariu C, Scorţanu E,  Prisăcariu V.A – “Characterization of some polyurethane elastomers with 1,4-butanediol

chain extender and dibenzyl derivatives”,  Bul. Inst. Polit. Iaşi, Tom LII (LVI), Fasc.2, 13-18, (2006)

33. Prisăcariu C, Scorţanu E –“Modifications induced by static tensile testings in polyurethanic films”, Bul. Inst. Polit.

Iaşi, Tom LII (LVI), Fasc. 2, 23-26, (2006).

35. Scorţanu, C. Prisacariu C, Hitruc E, Caraculacu A. – “New Heterocyclic Polyurethane-Ureas Based on 4,4'-

Dibenzyl Diisocyanate. 2. Infuence of Pyridine Units on the Mechanical Properties”  High  Perform. Polym. 18 (6),

877-891, (2006).

36. C Prisacariu, C.P. Buckley, A.A. Caraculacu – „Synthesis and characterization of novel shape memory

polyurethanes derived from 4,4'-dibenzyl diisocyanates, PU Deutsche Magazin ,4, 253- 258., (2006).

37. C. Prisacariu, E. Scortanu,- „ Stress-strain data of novel dibenzyl diisocyanate based polyurethane elastomers with

diamine chain extension” , DYFP 2006, 13th International Conference on Deformation, Yield and Fracture of

Polymers, Conf. Proceedings, 421 – 424, (2006)

38. C. Prisacariu– „The study of the evolution of mechanical deformation processes in casting polyurethane elastomers

under tensile load” , DYFP 2006, 13th International Conference on Deformation, Yield and Fracture of Polymers,

Conf. Proceedings, 425 – 428, (2006)

39. C. Prisacariu, A. Caraculacu, - „Selected thermoplastic dibenzyl based polyurethane blends with diol chain

extension: synthesis and characterization” , DYFP 2006, 13th International Conference on Deformation,  Yield and

Fracture of Polymers,  Conf. Proceedings, 450 – 453, (2006)

40. C. Prisacariu, C.P. Buckley,- „Influence of the type of chain extender and urethane group content in the

mechanical properties of polyurethanes based on 4,4’– dibenzyl diisocyanate”, DYFP 2006, 13th International

Conference on Deformation, Yield and Fracture of Polymers, Conf. Proceedings, 456 – 459, (2006)

41. C. Prisacariu, C.P. Buckley, A. Caraculacu, - „From phase separation to mechanical performance of novel

polyurethane elastomers derived from hard segments with a coplanar packing” , DYFP 2006, 13th International

Conference on Deformation, Yield and Fracture of Polymers, Conf. Proceedings, 482 – 485, (2006)

42. C.P. Buckley, C. Prisacariu, A. Caraculacu, - „ A new family of glassy polyurethanes and their performance as

shape-memory materials” , DYFP 2006, 13th International Conference on Deformation, Yield and Fracture of

Polymers, Conf. Proceedings, 284 – 287, (2006).

Year 2007

43. E. Scortanu, C. Prisacariu, „New aspects on the synthesis and properties of some azoxy- and  azo-group containing compounds”, - J. Optoelectron. Adv. Mater., Vol. 9, No. 4, 1025-1028,

(2007).

44. E. Scortanu, C. Prisacariu, “New aspects on the synthesis and properties of some azoxy- and azo-groups containing compounds”, J.Optoelectron.Adv.Mater. vol. 9, No 4, 1025-1028, (2007).

45. C. Prisacariu, E.Scortanu , Study of the compression properties of polyurethanes based on dibenzyl monomers and 1,4-butandiol as compared to other diol chain extenders, Rev. Roum. Chim., (2007), 52(1-2), 113-116.

46. Prisăcariu C., Caraculacu A., Scorţanu E., Hitruc G.H. Rev. Roum. Chim., “New Trends in The Synthesis and Properties of Polyurethanes Based on Dibenzyl Diisocyanate”, Rev. Roum. Chim., (2007), 52(4), 415-422.

47. C. Prisacariu, E. Scortanu, Crystallization and Properties of Novel Polyurethanes Based on the Chain Extender Ethylene Glycol and Aromatic Diisocyanates of Variable Flexibility,

Macromol. Symp., (2007), 254, 153-159.

48. C.P. Buckley, C. Prisacariu, A. Caraculacu, - „ Novel triol-crosslinked polyurethanes and their thermorheological characterization as shape-memory materials”, Polymer   48,  p.1388-1396 (2007)

49. C. Prisacariu, C.P. Buckley, - “Synthesis and Characterization of Some Novel Polyurethanes based on Rigid or Flexible Aromatic Diisocyanates and Mixtures of Them”, ANTEC Meeting, Cincinnati, USA, May 2007, p. 992-994.

50. C. Prisacariu, - “ New Polyurethanic Materials Derived from Dibenzyl Monomers: Elastomers, Films and Blends”, ANTEC Meeting, Cincinnati, USA, May 2007, p. 3132- 3135..

51. C. Prisacariu, E. Scortanu, "Infrared Dichroic studies of Phase Separation and Orientation of Dibenzyl Hard  Segments in Polyurethanes" (Ref# HPPJ 070118), published on 5.11.2007, available online High Performance Polymers - http://hip.sagepub.com/cgi/content/abstract/0954008307080750v1.

Chapters in Books – (Ed. Taylor & Francis)

Buckley C.P,  Prisacariu C,  Caraculacu, A., Martin C.M. - ”Inelasticity of hard-phase reinforced elastomers: A study of copolyurethanes with varying hard and soft segments”,

Constitutive Models for Rubber IV, Edited by P.-E. Austrell / L. Hari. ISBN 0415383463,  Ed. Taylor and Francis, 465 – 470, (2005).

Books

E. Scortanu, C. Prisacariu, A.A. Caraculacu,- “Contributions towards the field of polymers with thermal and photo-oxidative stability / “Contributii in domeniul polimerilor cu stabilitate termica si foto-oxidativa. Aplicatii”., Ed. Fides, ISBN 973-8930-08-1, publiched in November (2006).

ii. (b) SELECTIVE LIST OF LECTURES CONTRIBUTED AND INTERANTIONAL EVENTS

    - Experimental and theoretical studies on the relationship between chemical/physical properties and mechanical  performance of elastomeric polyurethanes"-C. PRISACARIU- invited lecture, Kick off Workshop, , în cadrul   programului ESF "Experimental and Theoretical Investigation of  Complex Polymer Structures (SUPERNET),   Strasbourg, 19-21, November 1999.

    - Investigation of complex polymer structures in the field of polyurethane elastomers  based on hard segments with variable geometry"- C. PRISACARIU –oral presentation, Cooperation Exchange 2000 Brokerage Event COPEX 2000, organizată în cadrul  Programului cadru V al Cordis, 5-6 June,Vienna 2000.

    - Physical and chemical aspects of classical and novel polyurethanes- C. PRISACARIU - lecture, Oxford Interdepartmental Polymer Seminars, 11 July 2000.

    - The optimization of polyurethane elastomers' mechanical properties- C. PRISACARIU  Oxford University  to representatives  of Oxford University, Keele University and industry (Huntsman Polyurethanes) –lecture, 20 July  2000.

    - The Effect of Structure on The Thermal and Mechanical Behaviour of PU based on hard segments with variable geometry - C. PRISACARIU-lecture, "The European Student Conference in Colloids and Polymers", Cardiff University, UK, 5-9 July 2000.

    - Mechanically Stress Induced Transformations in Dibenzyl Diisocyanate Based Polyurethane Elastomers" – C. PRISACARIU, A. Caraculacu- short lecture, "Polymeric Materials 2000" - Halle/Saale,Germania, 25 - 27 Sept 2000.

    - New Developments in The Structure - Property Relationship of Polyurethane Elastomers – C. PRISACARIU seminar, Institute of Polymer Research Dresden,Germany, 14 May 2001.

    - Characterization of Novel Complex Polymer Structures in The Field of Polyurethane Films and Blends –                C. PRISACARIU - seminar, Fakultat fur Phzsik und Geowissenschaften,Leipzig, Germany, 16 May 2001.

    - From Phase Separation to Morphology and  Mechanical Performance of Novel Polyurethanes  Based on Complex Hard Segments of Variable Geometry –C.PRISACARIU, - seminar,  School of Mechanical and Materials Eng.      University of Surrey, UK, 7 August 2001.

    - "Morphology of Polyurethane Elastomers and Blends", C. PRISACARIU - seminar, School of Chemistry and     Physics, Keele, University, UK, 9 August 2001.

    - C. PRISACARIU, C.P.Buckley, G.E.Hitruc şi A.A. Caraculacu,  Mechanical response of dibenzyl polyurethanes

with diol chain extenders,  lecture, la 11th International Conference in Polymers  and Organic Chemistry,

POC ’04, Prague, Czech Republic, 18-23 July, 2004.

    - PRISACARIU C. (lecture), “Thermal behaviour of selected polzurethane elastomers with diol chain extension”, 21

st Annual Meeting of The Polymer Processing Society, (PPS-21), Leipzig, Germany, 19-23 June 2005.

    - PRISACARIU C.  (plenary lecture), “A new approach to polymers based on isocyanates via an UK Royal Society

Joint Project between ‘Petru Poni’ Institute of Macromolecular Chemistry, Iasi and The University of Oxford, UK”,

The Fifth International Congress in Materials Science and Engineering, Iasi, 26-27 May, 2005

    - Prisacariu C., Caraculacu A., Scortanu E., Hitruc G.H. ( lecture) «NOUVELLES TENDANCES DANS LA

SYNTHESE ET LES PROPRIETES DES POLYMERES POLYURETHANIQUES A BASE DE 4, 4’

DIBENZYLE DIISOCYANATES, «7eme Colloque Franco-Roumain sur Les Polymeres », Iasi, 2-6 Septembrie

2005

    - Buckley C.P, Prisacariu C, Caraculacu A, Martin CM,  (lecture), “Inelasticity in the constitutive response of hard-

phase-reinforced elastomers: a study of copolyurethanes with varying hard and soft segments”, 4th European

Conference on Constitutive Models for Rubber, Stockholm, June 27-29, (2005).

  - Prisacariu C. Buckley C.P. Caraculacu A, ( lecture), -  “From phase separation to mechanical performance of

novel polyurethane elastomers derived from hard segments with a coplanar packing” , 13 th International

Conference of Deformation, Yield and Fracture of Polymers, (DYFP), Mastricht, The Netherlands, 9 – 13 April

2006.

18. Cristina Prisacariu, - “ On the Mechanical Properties Evolution of New Polyurethanes of Variable Controlled

Crystallinity – Structural Studies – Deuterated and Postcured Melt Cast Elastomers and Films with Dibenzyl

Structures” ,  - short lecture- SL-D8, Polymerwerkstoffe 2006, Halle/Salle, 27 - 29. September, 2006.

19. C. Prisacariu, C.P. Buckley, - “Synthesis and Characterization of Some Novel Polyurethanes based on Rigid or

Flexible Aromatic Diisocyanates and Mixtures of Them”, lecture,  ANTEC Meeting, Cincinnati, USA, May 2007.

20. C. Prisacariu, C.P. Buckley - “”Nanometer-Scale structural origins of mechanical properties of polyurethanes”,

special lecture 46th Miicrosymposium on Nanostructures Polymers and Polymer Nanocomposites, Prague, 8-12 July,

2007.

21  C. Prisacariu, C.P. Buckley, V.A. Prisacariu - “Mechanical response of Novel Crosslinked Thermoplastic

Polyurethane Elastomers Derived from Single and Mixtures od Isocyanates of Variable Geometry”-  special

lecture, 3rd International Symposium on “Reactive Polymers in Inhomogeneous Systems, in Melts ans at Interfaces”,

REACT 2007, Dredsen, Germany 23-26 Sept. 2007.

iii. Current work done as part of the NATO project.

As shown in my CV, starting year 2003 I have acted as a Romanian Project Leader of 4 national research grants and 2 international project as follows: a UK Royal Society Joint Project (2003 -2005) and an ongoing NATO Collaborative Linkage Grant, 2005 – 2008, project nr: PDD(CBP.EAP.CLG 981805/ 22.07.2005); both of them between The Institute of Macromolecular Chemistry “Petru Poni”, Iasi, Romania and The Department Engineering Science, University of  Oxford, UK with Professor Paul C. Buckley acting as the UK Co-director of these projects;

- title of the previous UK Royal Society Joint Project: “Optimising performance of polyurethanic products via control of chemical structure”

- title of the ongoing NATO project „ New polyurethanes and the nano-structural origin of their stress-strain response”.

The overall objective followed in these projects was/is mainly to improve understanding of the relationship between molecular/supramolecular architecture, and useful mechanical properties, for a uniquely versatile family of synthetic polymers consisting of: (a) conventional commercial polyurethanes; (b) novel Romanian polyurethanes (PU) and blends based on flexible hard segments of variable geometry; (c) novel deuterated PU; (d) nanopolyurethanes with new flexible hard segments, containing inorganic fillers; (e) new smart stimuli –responsive shape memory polyurethanic materials with large possible utilizations in civil and military applications . The goal was/is to enable molecular tailoring of these materials, to optimise their performance in a variety of practical applications. The approach is interdisciplinary, combining synthetic macromolecular chemistry at the Romanian Institute and microstuctural studies at Polymer Science Centre, University of Reading, UK, with the study and quantitative modelling of mechanical properties which was /is made and at The Engineering Science Department, Oxford University, UK. High strain rate experiments in PU are now studied at present at the Oxford department with the aim to find new applications in the survivability of our PU structures under impact loading, including those encountered in blast and ballistic events. The final outcome of this work is a predictive capability, whereby performance of these materials will be calculable for any given application, in terms of: their chemistry and microstructure and the form of the product. This is aimed at making a concerted study of the influence of nano-structural aspects (chemical and physical) on the mechanical performance of polyurethanes at an unprecedented level of detail (exploiting small-angle x-ray and neutron scattering and high resolution electron microscopy). Collaboration between the Romanian and British partners was/is making available to the researchers a uniquely rich set of polyurethanes with which to study systematically the role of nano-scale structural details in controlling elastomeric performance.

Therefore my research interests derive from these projects and are focused both on the investigation of conventional classical polyurethanes and on novel Romanian polyurethanic (PU) materials in the context of three important application areas for them: (a) their use as elastomeric materials with potential military/medical/ aerospace applications; (b) their use as nanopolyurethanes based on new flexible DBDI based hard segments, containing inorganic fillers; (c) new smart stimuli – responsive ‘shape-memory’ materials and their potential use in civil and military applications.